UNIT-I  
Introduction to Composite Materials
Composite Material: 

“A combination of two or more materials that results in better properties than those of the individual components used alone. In contrast to metallic alloys, each material retains its separate chemical, physical, and mechanical properties. The two constituents are reinforcement and a matrix. “

Advantages of composite materials: 
· High strength and stiffness, combined with low density, when compared with bulk materials, allowing for a weight reduction in the finished part. 
· The reinforcing phase provides the strength and stiffness. 
· In most cases, the reinforcement is harder, stronger, and stiffer than the matrix. 
· The reinforcement is usually a fiber or a particulate. 
· Particulate composites have dimensions that are approximately equal in all directions. 
· They may be spherical, platelets, or any other regular or irregular geometry. 
· Particulate composites tend to be much weaker and less stiff than continuous fiber composites, but they are usually much less expensive. 
· Particulate reinforced composites usually contain less reinforcement (up to 40 to 50 volume percent) due to processing difficulties and brittleness.
A fiber has a length that is much greater than its diameter. The length-to-diameter (l/d) ratio is known as the aspect ratio and can vary greatly. Continuous fibers have long aspect ratios, while discontinuous fibers have short aspect ratios. Continuous-fiber composites normally have a preferred orientation, while discontinuous fibers generally have a random orientation. Examples of continuous reinforcements include unidirectional, woven cloth, and helical winding (Fig. 1.1a), while examples of discontinuous reinforcements are chopped fibers and random mat (Fig. 1.1b). Continuous-fiber composites are often made into laminates by stacking single sheets of continuous fibers in different orientations to obtain the desired strength and stiffness properties with fiber volumes as high as 60 to 70 percent. Fibers produce high-strength composites because of their small diameter; they contain far fewer defects (normally surface defects) compared to the material produced in bulk. As a general rule, the smaller the diameter of the fiber, the higher its strength, but often the cost increases as the diameter becomes smaller. In addition, smaller-diameter high-strength fibers have greater flexibility and are more amenable to fabrication processes such as weaving or forming over radii. Typical fibers include glass, aramid, and carbon, which may be continuous or discontinuous. The continuous phase is the matrix, which is a polymer, metal, or ceramic. Polymers have low strength and stiffness, metals have intermediate strength and stiffness but high ductility, and ceramics have high strength and stiffness but are brittle. The matrix (continuous phase) performs several critical functions, including maintaining the fibers in the proper orientation and spacing and protecting them from abrasion and the environment. In polymer and metal matrix composites that form a strong bond between the fiber and the matrix, the matrix transmits loads from the matrix to the fibers through shear loading at the interface. In ceramic matrix composites, the objective is often to increase the toughness rather than the strength and stiffness; therefore, a low interfacial strength bond is desirable.

[image: image1.png]Continuous

Unidirectional (UD) Cloth
00000 950%-
o 0°/90° (Woven)
(a)

Roving

430° Helical
Filament Wound

Discontinuous

Chopped

(b)

1.1 Typicalreinforcement tpes

Mat




In matrix-based structural composites, the matrix serves two paramount purposes viz., binding the reinforcement phases in place and deforming to distribute the stresses among the constituent reinforcement materials under an applied force. 

The demands on matrices are many. They may need to temperature variations, be conductors or resistors of electricity, have moisture sensitivity etc. This may offer weight advantages, ease of handling and other merits which may also become applicable depending on the purpose for which matrices are chosen.  Solids that accommodate stress to incorporate other constituents provide strong bonds for the reinforcing phase are potential matrix materials. A few inorganic materials, polymers and metals have found applications as matrix materials in the designing of structural composites, with commendable success. These materials remain elastic till failure occurs and show decreased failure strain, when loaded in tension and compression. 

Composites cannot be made from constituents with divergent linear expansion characteristics. The interface is the area of contact between the reinforcement and the matrix materials. In some cases, the region is a distinct added phase. Whenever there is inter-phase, there has to be two inter-phases between each side of the inter-phase and its adjoint constituent. Some composites provide inter-phases when surfaces dissimilar constituents interact with each other. Choice of fabrication method depends on matrix properties and the effect of matrix on properties of reinforcements. One of the prime considerations in the selection and fabrication of composites is that the constituents should be chemically inert non-reactive. Figure 1.1 helps to classify matrices.

[image: image2.png]Matrices

l

i

1

I

l

Polymer
matrix
materials

Metal
matrix
materials

Ceramic
matrix
materials

Carbon and
Graphic matrix
materials

—

Thermosets

Thermoplastics

Fig.1.1





1.1.1 Polymer Matrix Materials 
Polymers make ideal materials as they can be processed easily, possess lightweight, and desirable mechanical properties. It follows, therefore, that high temperature resins are extensively used in aeronautical applications. 

Two main kinds of polymers are thermosets and thermoplastics. Thermosets have qualities such as a well-bonded three-dimensional molecular structure after curing. They decompose instead of melting on hardening. Merely changing the basic composition of the resin is enough to alter the conditions suitably for curing and determine its other characteristics. They can be retained in a partially cured condition too over prolonged periods of time, rendering Thermosets very flexible. Thus, they are most suited as matrix bases for advanced conditions fiber reinforced composites. Thermosets find wide ranging applications in the chopped fiber composites form particularly when a premixed or moulding compound with fibers of specific quality and aspect ratio happens to be starting material as in epoxy, polymer and phenolic polyamide resins. 

Thermoplastics have one- or two-dimensional molecular structure and they tend to at an elevated temperature and show exaggerated melting point. Another advantage is that the process of softening at 
elevated temperatures can reversed to regain its properties during cooling, facilitating applications of conventional compress techniques to mould the compounds. Resins reinforced with thermoplastics now comprised an emerging group of composites. The theme of most experiments in this area to improve the base properties of the resins and extract the greatest functional advantages from them in new avenues, including attempts to replace metals in die-casting processes. In crystalline thermoplastics, the reinforcement affects the morphology to a considerable extent, prompting the reinforcement to empower nucleation. Whenever crystalline or amorphous, these resins possess the facility to alter their creep over an extensive range of temperature. But this range includes the point at which the usage of resins is constrained, and the reinforcement in such systems can increase the failure load as well as creep resistance. Figure 1.2 shows kinds of thermoplastics
.
[image: image3.png]Thermoplastics

v
l l | !
Polyethylene | | Polystyrene Polyamides | | Nylons | | Polyropylenc





A small quantum of shrinkage and the tendency of the shape to retain its original form are also to be accounted for. But reinforcements can change this condition too. The advantage of thermoplastics systems over thermosets are that there are no chemical reactions involved, which often result in the release of gases or heat. Manufacturing is limited by the time required for heating, shaping and cooling the structures. 

Thermoplastics resins are sold as moulding compounds. Fiber reinforcement is apt for these resins. Since the fibers are randomly dispersed, the reinforcement will be almost isotropic. However, when subjected to moulding processes, they can be aligned directionally. 

There are a few options to increase heat resistance in thermoplastics. Addition of fillers raises the heat resistance. But all thermoplastic composites tend loose their strength at elevated temperatures. However, their redeeming qualities like rigidity, toughness and ability to repudiate creep, place thermoplastics in the important composite materials bracket. They are used in automotive control panels, electronic products encasement etc. 

Newer developments augur the broadening of the scope of applications of thermoplastics. Huge sheets of reinforced thermoplastics are now available and they only require sampling and heating to be moulded into the required shapes. This has facilitated easy fabrication of bulky components, doing away with the more cumbersome moulding compounds. 

Thermosets are the most popular of the fiber composite matrices without which, research and development in structural engineering field could get truncated. Aerospace components, automobile parts, defense systems etc., use a great deal of this type of fiber composites. Epoxy matrix materials are used in printed circuit boards and similar areas. Figure 1.3 shows some kinds of thermosets.

[image: image4.png]Thermosets

v

]

Phenolic polyamide
resins

Polyester





Direct condensation polymerization followed by rearrangement reactions to form heterocyclic entities is the method generally used to produce thermoset resins. Water, a product of the reaction, in both methods, hinders production of void-free composites. These voids have a negative effect on properties of the composites in terms of strength and dielectric properties. Polyesters phenolic and Epoxies are the two important classes of thermoset resins. 

Epoxy resins are widely used in filament-wound composites and are suitable for moulding prepress. They are reasonably stable to chemical attacks and are excellent adherents having slow shrinkage during curing and no emission of volatile gases. These advantages, however, make the use of epoxies rather expensive. Also, they cannot be expected beyond a temperature of 140ºC. Their use in high technology areas where service temperatures are higher, as a result, is ruled out. 

Polyester resins on the other hand are quite easily accessible, cheap and find use in a wide range of fields. Liquid polyesters are stored at room temperature for months, sometimes for years and the mere addition of a catalyst can cure the matrix material within a short time. They are used in automobile and structural applications. 

The cured polyester is usually rigid or flexible as the case may be and transparent. Polyesters withstand the variations of environment and stable against chemicals. Depending on the formulation of the resin or service requirement of application, they can be used up to about 75ºC or higher. Other advantages of polyesters include easy compatibility with few glass fibers and can be used with verify of reinforced plastic accountrey. 

Aromatic Polyamides are the most sought after candidates as the matrices of advanced fiber composites for structural applications demanding long duration exposure for continuous service at around 200-250ºC .
1.1.2 Metal Matrix Materials 
Metal matrix composites, at present though generating a wide interest in research fraternity, are not as widely in use as their plastic counterparts. High strength, fracture toughness and stiffness are offered by metal matrices than those offered by their polymer counterparts. They can withstand elevated temperature in corrosive environment than polymer composites. Most metals and alloys could be used as matrices and they require reinforcement materials which need to be stable over a range of temperature and non-reactive too. However the guiding aspect for the choice depends essentially on the matrix  material. Light metals form the matrix for temperature application and the reinforcements in addition to the aforementioned reasons are characterized by high moduli. 

Most metals and alloys make good matrices. However, practically, the choices for low temperature applications are not many. Only light metals are responsive, with their low density proving an advantage. Titanium, Aluminium and magnesium are the popular matrix metals currently in vogue, which are particularly useful for aircraft applications. If metallic matrix materials have to offer high strength, they require high modulus reinforcements. The strength-to-weight ratios of resulting composites can be higher than most alloys. 

The melting point, physical and mechanical properties of the composite at various temperatures determine the service temperature of composites. Most metals, ceramics and compounds can be used with matrices of low melting point alloys. The choice of reinforcements becomes more stunted with increase in the melting temperature of matrix materials. 

1.1.3 Ceramic Matrix Materials 
Ceramics can be described as solid materials which exhibit very strong ionic bonding in general and in few cases covalent bonding. High melting points, good corrosion resistance, stability at elevated temperatures and high compressive strength, render ceramic-based matrix materials a favourite for applications requiring a structural material that doesn’t give way at temperatures above 1500ºC. Naturally, ceramic matrices are the obvious choice for high temperature applications. 

High modulus of elasticity and low tensile strain, which most ceramics posses, have combined to cause the failure of attempts to add reinforcements to obtain strength improvement. This is because at the stress levels at which ceramics rupture, there is insufficient elongation of the matrix which keeps composite from transferring an effective quantum of load to the reinforcement and the composite may fail unless the percentage of fiber volume is high enough. A material is reinforcement to utilize the higher tensile strength of the fiber, to produce an increase in load bearing capacity of the matrix. Addition of high-strength fiber to a weaker ceramic has not always been successful and often the resultant composite has proved to be weaker. 

The use of reinforcement with high modulus of elasticity may take care of the problem to some extent and presents pre-stressing of the fiber in the ceramic matrix is being increasingly resorted to as an option. 

When ceramics have a higher thermal expansion coefficient than reinforcement materials, the resultant composite is unlikely to have a superior level of strength. In that case, the composite will develop strength within ceramic at the time of cooling resulting in microcracks extending from fiber to fiber within the matrix. Microcracking can result in a composite with tensile strength lower than that of the matrix. 

1.1.4 Carbon Matrices 
Carbon and graphite have a special place in composite materials options, both being highly superior, high temperature materials with strengths and rigidity that are not affected by temperature up to 2300ºC. 

This carbon-carbon composite is fabricated through compaction of carbon or multiple impregnations of porous frames with liquid carboniser precursors and subsequent pyrolization. They can also be manufactured through chemical vapour deposition of pyrolytic carbon. Carbon-carbon composites are not be applied in elevated temperatures, as many composites have proved to be far superior at these temperatures. However, their capacity to retain their properties at room temperature as well as at temperature in the range of 2400ºC and their dimensional stability make them the oblivious choice in a garnut of applications related to aeronautics, military, industry and space.  Components, that are exposed to higher temperature and on which the demands for high standard performance are many, are most likely to have carbon-carbon composites used in them. 

1.1.5 Glass Matrices 
I n comparison to ceramics and even considered on their own merit, glass matrices are found to be more reinforcement-friendly. The various manufacturing methods of polymers can be used for glass matrices. 

Glasses are meant to improve upon performance of several applications. Glass matrix composite with high strength and modulus can be obtained and they can be maintained upto temperature of the order of 650ºC. 

Composites with glass matrices are considered superior in dimensions to polymer or metal system, due to the low thermal expansion behaviour. This property allows fabrication of many components in intricate shapes and their tribological characters are considered very special. Since the elastic modulus of glass is far lower than of any prospective reinforcement materials, application of stress usually results in high elasticity modulus fiber that the tensile strength of the composite its considerably enhanced than that of the constituents, which is not case in ceramic matrices.

[image: image5.png]Reinforcements.

|

I

]

I
!

]

}

Fibres

Filled

‘Whiskers Flake

Particulates

l—¢—l

Particle filled

Microsperes

l—¢—l

Solid

Hollow

Directionally
Solidified
eutectics





Reinforcing constituents in composites, as the word indicates, provide the strength that makes the composite what it is. But they also serve certain additional purposes of heat resistance or conduction, resistance to corrosion and provide rigidity. Reinforcement can be made to perform all or one of these functions as per the requirements. 

A reinforcement that embellishes the matrix strength must be stronger and stiffer than the matrix and capable of changing failure mechanism to the advantage of the composite. This means that the ductility should be minimum or even nil the composite must behave as brittle as possible. 

1.1.7 Fiber Reinforcement 
Fibers are the important class of reinforcements, as they satisfy the desired conditions and transfer strength to the matrix constituent influencing and enhancing their properties as desired. 

Glass fibers are the earliest known fibers used to reinforce materials. Ceramic and metal fibers were subsequently found out and put to extensive use, to render composites stiffer more resistant to heat. 

Fibers fall short of ideal performance due to several factors. The performance of a fiber composite is judged by its length, shape, and orientation, composition of the fibers and the mechanical properties of the matrix. 

The orientation of the fiber in the matrix is an indication of the strength of the composite and the strength is greatest along the longitudinal directional of fiber. This doesn’t mean the longitudinal fibers can take the same quantum of load irrespective of the direction in which it is applied. Optimum performance from longitudinal fibers can be obtained if the load is applied along its direction. The slightest shift in the angle of loading may drastically reduce the strength of the composite.  Unidirectional loading is found in few structures and hence it is prudent to give a mix of orientations for fibers in composites particularly where the load is expected to be the heaviest. 

Monolayer tapes consisting of continuous or discontinuous fibers can be oriented unidirectional stacked into plies containing layers of filaments also oriented in the same direction. More complicated orientations are possible too and nowadays, computers are used to make projections of such variations to suit specific needs. In short, in planar composites, strength can be changed from unidirectional fiber oriented composites that result in composites with nearly isotropic properties. 

Properties of angle-plied composites which are not quasi-isotropic may vary with the number of plies and their orientations. Composite variables in such composites are assumed to have a constant ratio and the matrices are considered relatively weaker than the fibers. The strength of the fiber in any one of the three axes would, therefore be one-third the unidirectional fiber composite, assuming that the volume percentage is equal in all three axes. 

However, orientation of short fibers by different methods is also possible like random orientations by sprinkling on to given plane or addition of matrix in liquid or solid state before or after the fiber deposition. Even three-dimensional orientations can achieve in this way. There are several methods of random fiber orientations, which in a two-dimensional one, yield composites with one-third the strength of an unidirectional fiber-stressed composite, in the direction of fibers. In a 3-dimension, it would result in a composite with a comparable ratio, about less than one-fifth. 

In very strong matrices, moduli and strengths have not been observed. Application of the strength of the composites with such matrices and several orientations is also possible. The longitudinal strength can be calculated on the basis of the assumption that fibers have been reduced to their effective strength on approximation value in composites with strong matrices and non-longitudinally orientated fiberss. 

It goes without saying that fiber composites may be constructed with either continuous or short fibers. Experience has shown that continuous fibers (or filaments) exhibit better orientation, although it does not reflect in their performance. Fibers have a high aspect ratio, i.e., their lengths being several times greater than their effective diameters. This is the reason why filaments are manufactured using continuous process. This finished filaments. 

Mass production of filaments is well known and they match with several matrices in different ways like winding, twisting, weaving and knitting, which exhibit the characteristics of a fabric. 

Since they have low densities and high strengths, the fiber lengths in filaments or other fibers yield considerable influence on the mechanical properties as well as the response of composites to processing and procedures. Shorter fibers with proper orientation composites that use glass, ceramic or multi-purpose fibers can be endowed with considerably higher strength than those that use continuous fibers. Short fibers are also known to their theoretical strength. The continuous fiber constituent of a composite is often joined by the filament winding process in which the matrix impregnated fiber wrapped around a mandrel shaped like the part over which the composite is to be placed, and equitable load distribution and favorable orientation of the fiber is possible in the finished product. However, winding is mostly confined to fabrication of bodies of revolution and the occasional irregular, flat surface.  Short-length fibers incorporated by the open- or close-mould process are found to be less efficient, although the input costs are considerably lower than filament winding. 

Most fibers in use currently are solids which are easy to produce and handle, having a circular cross-section, although a few non-conventional shaped and hollow fibers show signs of capabilities that can improve the mechanical qualities of the composites. 

Given the fact that the vast difference in length and effective diameter of the fiber are assets to a fiber composite, it follows that greater strength in the fiber can be achieved by smaller diameters due to minimization or total elimination of surface of surface defects. 

After flat-thin filaments came into vogue, fibers rectangular cross sections have provided new options for applications in high strength structures. Owing to their shapes, these fibers provide perfect packing, while hollow fibers show better structural efficiency in composites that are desired for their stiffness and compressive strengths. In hollow fibers, the transverse compressive strength is lower than that of a solid fiber composite whenever the hollow portion is more than half the total fiber diameter. However, they are not easy to handle and fabricate. 

1.1.8Types of Fibers 
Organic and inorganic fibers are used to reinforce composite materials. Almost all organic fibers have low density, flexibility, and elasticity. Inorganic fibers are of high modulus, high thermal stability and possess greater rigidity than organic fibers and not withstanding the diverse advantages of organic fibers which render the composites in which they are used. 

Mainly, the following different types of fibers namely, glass fibers, silicon carbide fibers, high silica and quartz fibers, aluminina fibers, metal fibers and wires, graphite fibers, boron fibers, aramid fibers and multiphase fibers are used. Among the glass fibers, it is again classified into E-glass, A-glass, R-glass etc. There is a greater marker and higher degree of commercial movement of organic fibers. 

The potential of fibers of graphite, silica carbide and boron are also exercising the scientific mind due to their applications in advanced composites. 

1.1.8.1 Glass fibers 
Over 95% of the fibers used in reinforced plastics are glass fibers, as they are inexpensive, easy to manufacture and possess high strength and stiffness with respect to the plastics with which they are reinforced. Their low density, resistance to chemicals, insulation capacity are other bonus characteristics, although the one major disadvantage in glass is that it is prone to break when subjected to high tensile stress for a long time. 

However, it remains break-resistant at higher stress-levels in shorter time frames. This property mitigates the effective strength of glass especially when glass is expected to sustain loads for many months or years continuously. 

Period of loading, temperature, moisture and other factors also dictate the tolerance levels of glass fibers and the disadvantage is further compounded by the fact that the brittleness of glass does not make room for prior warning before the catamorphic failure. But all this can be easily overlooked in view of the fact the wide range of glass fiber variety lend themselves amicably to fabrication processes like matched die-moulding, filament winding lay-up and so on. Glass fibers are available in the form of mates, tapes, cloth, continuous and chopped filaments, roving and yarns. Addition of chemicals to silica sand while making glass yields different types of glasses. 

1.1.8.2 Metals fibers 
As reinforcement, metal fibers have many advantages. They are easily produced using several fabrication processes and are more ductile, apart from being not too sensitive to surface damage and possess high strengths and temperature resistance. However, their weight and the tendency to react each other through alloying mechanisms are major disadvantages. Ceramic fibers improve vastly in performance when a fine metal outline is incorporated with refractory ceramics by improving their thermal shock and impact resistance properties. Metal wires, of the continuous version, also reinforce plastics like polyethylene and epoxy. Such combinations ensure high strength, light weight and good fatigue resistance. 

Besides, continuous metal fibers are easily handled, unlike glass fibers. Better flexural properties are observed in some metal fibers reinforced plastic composites which also offer improved strength and weight, than glass fibers. However, their poor tolerance of high temperature and the resultant steep variations of thermal expansion coefficient with the resins are a discouragement that limits their their application. 

1.1.8.3 Alumina Fibers 
Alumina aluminium oxide fibers, basically developed for use in metal matrices are considered a potential resin-matrix composite reinforcement. It offers good compressive strength rather than tensile strength. It’s important property is it’s high melting point of about 2000ºC and the composite can be successfully used at temperature up to about 1000ºC. Magnesium and aluminum matrices frequently use alumina fiber reinforced composites as they do not damage the fiber even in the liquid state. 

1.1.8.4 Boron Fibers 
They are basically composites, in which boron is coated on a substance which forms the substrate, usually made of tungsten. Boron-tungsten fibers are obtained by allowing hot tungsten filament through a mixture of gases. Boron is deposited on tungsten and the process continued until the thickness is achieved. The tungsten however remains constant in its thickness. 

Properties of boron fibers generally change with the diameter, because of the changing ratio of boron to tungsten and the surface defects that change according to size. However, they are known for their remarkable stiffness and strength. Their strengths often compare with those of glass fibers, but their tensile modulus is high, almost four to five that of glass. Boron coated carbons are much cheaper to make than boron tungsten fiber. But is low modulus of elasticity often works against it. 

1.1.8.5 Silicon Carbide fibers 
Silicon carbide can be coated over a few metals and their room temperature tensile strengths and tensile moduli are like those boron-tungsten. The advantages of silicon carbide-tungsten are several and are more desirable than uncoated boron tungsten fibers. Elevated temperature performance and the fact that they reported only a 35% loss of strength at 1350ºC are their best qualities. Silicon carbide-tungsten and silicon carbide-carbon have both been seen to have very high stress-rupture strength at 1100ºC and 1300ºC. Uncoated boron-tungsten fibers do not react with molten aluminum, unlike uncoated boron and they also withstand high temperatures used in hot-press titanium matrices. 

However, Silicon carbide-tungsten fibers are dense compared to boron-tungsten fibers of the same diameters. They are prone to surface damage and need careful, delicate handling, especially during fabrication of the composite. Further, above 930ºC weakening reactions occur between tungsten and silicon carbide, making it different to maintain balance in high-temperature matrix formations. 

Silicon carbide on carbon substrates have several advantages, viz. no reaction at high temperature, being lighter than silicon carbide tungsten and possessing tensile strengths and modulus that is are often better than those of silicon carbide-tungsten and boron fibers. 

1.1.8.6 Aramid Fibers 
Aramid fibers are made aromatic polyamides which are long polymeric chains and aromatic rings. They are structures in which six carbon s\atoms are bonded to each other and to combinations of hydrogen atoms. In aramid fibers, these rings occur and reoccur to form the fibers. They were initially used to reinforce automobile tires. Since then, they have also found other uses like bullet proof vests. As high strength applications, their use in power boats is not uncommon. 

Aramids have high tensile strength, high modulus and low weight. Impact-resistant structures can be produced from aramids. The density of aramid fibers is less than that of glass and graphite fibers. They are fire resistant apart from being high-temperature resistant and unaffected by organic solvents fuels. But their resistance in acid and alkaline media is poor. They are supple and allow themselves to be woven into matrices by simple processes. Aramid fibers have a negative coefficient of thermal expansion in the fiber direction and failure of aramid fibers is unique. When they fail, the fibers break into small fibers, which are like fibers within the fibers. This unique failure mechanism is responsible for high strength. 

1.1.8.7 Quartz and Silica Fibers 
The glass-types typically contain about 50 to 70% silica. Silica glass is a purer glass fiber that can be made by treating fiberglass in an acid bath, which removes all impurities without affecting the silica. The final product contains 93 to 99% silica. Quartz is even more pure, and quartz fibers are made from natural quartz crystals that contain 99.9% silica, possessing nearly all the properties of pure solid quartz. 

Ordinary fiberglass, high silica and quartz fibers share several characteristics and can be produced in a range of fiber diameter. Roving or yarns and other forms of fibers can be made from high silica as well as quartz too. 

They differ from glass in many factors, however, especially in heat-related properties. 

Although quartz crystals are commonly available, pure crystals are hard to come by. On the other hand, high silica comes from the same material as glass fibers and is easily accessible. However, quartz makes up for its rarity with its capacity to withstand high temperatures, which silica is incapable of. 

Barring this difference, silica and quartz are similar in other respects. They are highly elastic and can be stretched to 1% of their length before break point. Both silica and quartz are not affected by acid attacks and are resistant to moisture. Owing to their thermal properties, silica and quartz are the natural choice as fibers in several applications. They have good insulting properties and do not melt at temperature up to 1600ºC. In addition, they have a low thermal expansion coefficient which makes them withstand high temperatures. 

1.1.8.8 Graphite Fibers 
While use of the term carbon for graphite is permissible, there is one basic difference between the two. Element analysis of poly-acrylo-nitrile (PAN) base carbon fibers show that they consist of 91 to 94% carbon. But graphite fibers are over 99% carbon. The difference arises from the fact that the fibers are made at different temperatures.  PAN-based carbon cloth or fiber is produced at about 1320ºC, while graphite fibers and cloth are graphitised at 1950 to 3000ºC.  The properties of graphite remain unchanged even at high temperatures, but its willingness to react readily with most metals at the fabrication stage or during use at very high temperatures is often a stumbling block, as seen in aluminium matrices when carbides are produced at the interface. These carbides react with moisture with disastrous effects on the composite material. 

Graphite fibers are some of the stiffer fibers known. The stiffness of the fiber is as high as the graphite content. But a major drawback is that stiffness and strength are inversely proportional to each other. Forbidding costs make the use of graphite fibers prohibitive. The best glass fibers are far less expensive than the cheapest, lowest quality of graphite, and in PAN-base fibers, other raw materials too are equally expensive. The carbonization and graphitisation are time-consuming, apart from demanding excessive energy, materials and close controls throughout the process. Cheaper pitch base fiber are now being developed, with greater performance potential and there are possibilities of the increased use of graphite fibers. 

1.1.8.9 Multiphase Fibers 
Spoolable filaments made by chemical vapour deposition processes are usually the multiphase variety and they usually comprise materials like boron, silicon and their carbides formed on surface of a very fine filament substrate like carbon or tungsten. They are usually good for high temperature applications, due to their reduced reaction with higher melting temperature of metals than graphite and other metallic fibers. Boron filaments are sought after for structural and intermediate-temperature composites. A poly-phase fiber is a core-sheath fiber consisting of a poly-crystalline core. 

1.1.9 Whiskers 
Single crystals grown with nearly zero defects are termed whiskers. They are usually discontinuous and short fibers of different cross sections made from several materials like graphite, silicon carbide, copper, iron etc. Typical lengths are in 3 to 55 N.M. ranges. Whiskers differ from particles in that, whiskers have a definite length to width ratio greater than one. Whiskers can have extraordinary strengths upto 7000 MPa. 

Whiskers were grown quite incidentally in laboratories for the first time, while nature has some geological structures that can be described as whiskers. Initially, their usefulness was overlooked as they were dismissed as incidental by-products of other structure. However, study on crystal structures and growth in metals sparked off an interest in them, and also the study of defects that affect the strength of materials, they came to be incorporated in composites using several methods, including power metallurgy and slip-casting techniques. 

Metal-whisker combination, strengthening the system at high temperatures, has been demonstrated at the laboratory level. But whiskers are fine, small sized materials not easy to handle and this comes in the way of incorporating them into engineering materials to come out with a superior quality composite system. 

Early research has shown that whisker strength varies inversely with effective diameter. When whiskers were embedded in matrices, whiskers of diameter upto 2 to 10μm yielded fairly good composites. 

Ceramic material’s whiskers have high moduli, useful strengths and low densities. Specific strength and specific modulus are very high and this makes ceramic whiskers suitable for low weight structure composites. They also resist temperature, mechanical damage and oxidation more responsively than metallic whiskers, which are denser than ceramic whiskers. However, they are not commercially viable because they are damaged while handling

1.2 CLASSIFICATION OF COMPOSITES 
1.2.1 Classification 
Composite materials are commonly classified at following two distinct levels: 

• The first level of classification is usually made with respect to the matrix constituent. The major composite classes include Organic Matrix Composites (OMCs), Metal Matrix Composites (MMCs) and Ceramic Matrix Composites (CMCs). The term organic matrix composite is generally assumed to include two classes of composites, namely Polymer Matrix Composites (PMCs) and carbon matrix composites commonly referred to as carbon-carbon composites. 

• The second level of classification refers to the reinforcement form - fibre reinforced composites, laminar composites and particulate composites. Fibre reinforced composites can be further divided into those containing discontinuous or continuous fibres. 

• Fibre Reinforced Composites are composed of fibres embedded in matrix material. Such a composite is considered to be a discontinuous fibre or short fibre composite if its properties vary with fibre length. On the other hand, when the length of the fibre is such that any further increase in length does not further increase, the elastic modulus of the composite, the composite is considered to be continuous fibre reinforced. Fibres are small in diameter and when pushed axially, they bend easily although they have very good tensile properties. These fibres must be supported to keep individual fibres from bending and buckling. 

• Laminar Composites are composed of layers of materials held together by matrix. Sandwich structures fall under this category. 

• Particulate Composites are composed of particles distributed or embedded in a matrix body. The particles may be flakes or in powder form. Concrete and wood particle boards are examples of this category. 

 Major processing routes for polymer matrix composites: 

Two types of polymer matrices are shown: thermosets and thermoplastics. A thermoset starts as a low-viscosity resin that reacts and cures during processing, forming an intractable solid. A thermoplastic is a high-viscosity resin that is processed by heating it above its melting temperature. Because a thermoset resin sets up and cures during processing, it cannot be reprocessed by reheating. By comparison, a thermoplastic can be reheated above its melting temperature for additional processing. There are processes for both classes of resins that are more amenable to discontinuous fibers and others that are more amenable to continuous fibers. In general, because metal and ceramic matrix composites require very high temperatures and sometimes high pressures for processing, they are normally much more expensive than polymer matrix composites. However, they have much better thermal stability, a requirement in applications where the composite is exposed to high temperatures. This book will deal with both continuous and discontinuous polymer, metal, and ceramic matrix
[image: image6.png]Composites
Processing
r
Thermaset Composites [Thermoplastc Composites|
Processing Processing
—I—\w —————
Short-Fiber Continuous Fiber ‘Short-Fiber Cantinuous Fiber
Composites Composites Composites Composites
Injection Molding Lay-Up Injection Molding Lay-Up
Compression Molding Filament Winding Compression Molding | | Thermoforming
Liquid Molding Liquid Mokding Compression Molding
Spray-Up. Pultrusion

Fig. 1.3 Majorpolymer matix compostie abrication processes




Elastic constants for anisotropic, orthotropic and isotropic materials.

Materials can be classified as either isotropic or anisotropic. Isotropic materials have the same material properties in all directions, and normal loads create only normal strains. By comparison, anisotropic materials have different material properties in all directions at a point in the body. There are no material planes of symmetry, and normal loads create both normal strains and shear strains. A material is isotropic if the properties are independent of direction within the material. For example, consider the element of an isotropic material shown in Fig. 1.4. If the material is loaded along its 0°, 45°, and 90° directions, the modulus of elasticity (E) is the same in each

direction (E0° E45° E90°). However, if the material is anisotropic (for example, the composite ply shown in Fig. 1.5), it has properties that vary with direction within the material. In this example, the moduli are different in each direction (E0° ≠E45° ≠E90°). While the modulus of elasticity is used in the example, the same dependence on direction can occur for other material properties, such as ultimate strength, Poisson’s ratio, and thermal expansion coefficient.

Bulk materials, such as metals and polymers, are normally treated as isotropic materials, while composites are treated as anisotropic. However, even bulk materials such as metals can become anisotropic––for example, if they are highly cold worked to produce grain alignment in a certain direction.

[image: image7.png]ig. 1.4 Element o soropic material under sress




Advantages and Disadvantages of Composite Materials
Advantages: 
1. lighter weight, 
2. the ability to tailor the layup for optimum strength and stiffness,
3.  improved fatigue life, 
4. corrosion resistance, and, 
5. With good design practice, reduced assembly costs due to fewer detail parts and fasteners. 
6. The specific strength (strength/density) and specific modulus (modulus/density) of highstrength fibers (especially carbon) are higher than those of other comparable aerospace metallic alloys (Fig. 1.18). 
7. This translates into greater weight savings resulting in improved performance, greater payloads, longer range, and fuel savings. 
8. Figure 1.19 compares the overall structural efficiency of carbon/epoxy, Ti-6Al-4V, and 7075-T6 aluminum. The chief engineer of aircraft structures for the U.S. Navy once told the author that he liked composites because “they don’t rot [corrode] and they don’t get tired [fatigue].” Corrosion of aluminum alloys is a major cost and a constant maintenance problem for both commercial and military aircraft. The corrosion resistance of composites can result in major savings in supportability costs. Carbon fiber composites cause galvanic corrosion of aluminum if the fibers are placed in direct contact with the metal surface, but bonding a glass fabric electrical insulation layer on all interfaces that contact aluminum eliminates this problem. The fatigue

Disadvantages: 

1. high raw material costs and usually high fabrication and assembly costs; 
2. adverse effects of both temperature and moisture; 
3. poor strength in the out-ofplane direction 
4. greater difficulty in repairing them compared to metallic structures.

5. The major cost driver in fabrication for a composite part using conventional hand lay-up is the 
cost of laying up or collating the plies. 
6. This cost is generally 40 to 60 percent of the fabrication cost, depending on part complexity (Fig. 1.21).

7. Assembly cost is another major cost driver, accounting for about 50 percent of the total part cost.
8. Temperature has an effect on composite mechanical properties. Typically, matrix-dominated

mechanical properties decrease with increasing temperature. 
9. Fiber-dominated properties are somewhat affected by cold temperatures, but the effects are not as severe as those of elevated temperature on the matrix-dominated properties.

 Applications

1. Applications include aerospace, transportation, construction, marine goods, sporting goods, and more recently infrastructure, with construction and transportation being the largest.

2. In general, high-performance but more costly continuous-carbon-fiber composites are used where high strength and stiffness along with light weight are required, and much lower-cost fiberglass composites are used in less demanding applications where weight is not as critical.

3. In military aircraft, low weight is “king” for performance and payload reasons, and composites often approach 20 to 40 percent of the airframe weight (Fig. 1.25). 

4. For decades, helicopters have incorporated glass fiber–reinforced rotor blades for improved fatigue resistance, and in recent years helicopter airframes have been built largely of carbon-fiber composites.

5. Military aircraft applications, the first to use highperformance continuous-carbon-fiber composites,

drove the development of much of the technology now being used by other industries.

6.  Both small and large commercial aircraft rely on composites to decrease weight and increase fuel performance, the most striking example being the 50 percent composite airframe for the new Boeing 787

(Fig. 1.26). 

7. All future Airbus and Boeing aircraft will use large amounts of high-performance composites. Composites are also used extensively in both weight-critical reusable and expendable launch vehicles and satellite structures (Fig. 1.27). 

8. Weight savings due to the use of composite materials in aerospace applications generally range from 15 to 25 percent. 
9. The major automakers (Fig. 1.28) are increasingly turning to composites to help them meet performance and weight requirements, thus improving fuel efficiency. Cost is a major driver for commercial  transportation, and composites offer lower weight and lower maintenance costs. Typical materials are fiberglass/ polyurethane made by liquid or compression molding and fiberglass/ polyester made by  compression molding. Recreational vehicles have long used glass fibers, mostly for their durability and weight savings over metal. The product form is typically fiberglass sheet molding compound made by compression molding. For high-performance Formula 1 racing cars, where cost is not an impediment, most of the chassis, including the monocoque, suspension, wings, and engine cover, is made from carbon fiber composites.

10. Corrosion is a major headache and expense for the marine industry. Composites help minimize these problems, primarily because they do not corrode like metals or rot like wood. Hulls of boats ranging from small fishing boats to large racing yachts (Fig. 1.29) are routinely made of glass fibers and polyester or vinyl ester resins. Masts are frequently fabricated from carbon fiber composites. Fiberglass filament-wound SCUBA proving the marine industry. 

11. Lighter tanks can hold more air yet require less maintenance than their metallic counterparts. Jet skis and boat trailers often contain glass composites to help minimize weight and reduce corrosion. 

12. More recently, the topside structures of many naval ships have been fabricated from composites.

13. Using composites to improve the infrastructure (Fig. 1.30) of our roads and bridges is a relatively

new, exciting application.

14.  Many of the world’s roads and bridges are badly corroded and in need of continual maintenance or replacement.

15. In the United States alone, it is estimated that more than 250,000 structures, such as bridges and parking garages, need repair, retrofit, or replacement. Composites offer much longer life with less maintenance due to their corrosion resistance. Typical processes/materials include wet lay-up repairs and corrosion-resistant fiberglass pultruded products
16. Wind power is the world’s fastest-growing energy source. The blades for large wind turbines (Fig. 1.32) are normally made of composites to improve electrical energy generation efficiency. These blades can be as long as 120 ft (37 m) and weigh up to 11,500 lb (5200 kg). In 2007, nearly 50,000 blades for 17,000 turbines were delivered, representing roughly 400 million pounds (approximately 180 million kg) of composites. The predominant material is continuous glass fibers manufactured by either lay-up or resin

infusion.

17. Tennis racquets (Fig. 1.33) have been made of glass for years, and many golf club shafts are made of carbon. Processes include compression molding for tennis racquets and tape wrapping or filament winding for golf shafts. Lighter, stronger skis and surfboards also are possible using composites. 
18. Another example of a composite application that takes a beating yet keeps on performing is a snowboard, which typically involves the use of a sandwich construction (composite skins with a honeycomb core) for maximum specific stiffness
